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SECTION 10 22 46 – FREESTANDING GLASS PARTITIONS
	GENERAL
	SUBMITTALS
	Action Submittals:
	Shop Drawings: Illustrate products, installation, and relationship to adjacent construction.
 	Product Data: Manufacturer’s descriptive data and product attributes.
 	Informational Submittals:
 	Certificate of Compliance: Certification that installed products meet specified design and performance requirements.
	SYSTEM DESCRIPTION
	Design Requirements:
	Live and dead loads: In accordance with [ASCE 7.] [Building Code.] [____.]
	QUALITY ASSURANCE
	Installer Qualifications: Firm specializing in work of this Section with minimum [2] [__] years’ experience.	Comment by ZeroDocs: Retain this paragraph to specify minimum installer qualifications.
	Mockup: [Minimum [4] [__] feet long x full height.] [____.] Approved mockup [may] [may not] remain as part of the Work.	Comment by ZeroDocs: Retain this paragraph for a full-size mockup.
	PRODUCTS
	MANUFACTURERS
	Contract Documents are based on Klarity Freestanding Glass Partition System by C.R. Laurence Co., Inc. www.crlaurence.com 
	Substitutions: [Refer to Division 01.] [Not permitted.]	Comment by ZeroDocs: Edit this paragraph to indicate whether substitutions will be allowed for the products in this section.
	MATERIALS
	Stainless Steel: ASTM A666, Type 316.
	Glass: ASTM C1172 and ANSI Z97.1, nominally 9/16 inch thick [clear] [[____] tinted] laminated with exposed edges polished, consisting of two layers of ¼ inch thick fully tempered glass with 0.060 inch thick interlayer.	Comment by ZeroDocs: In accordance with the IBC, glass has been designed using a safety factor of 4 in determining allowable flexural stress (6000 PSI). 
	FABRICATION
 	Partition Height: [[6] [7] [8] feet.] [As indicated.]	Comment by ZeroDocs: Maximum partition height is 8 feet with a maximum post spacing of 5 feet on center.
 	Posts: 
	Post height: [5] [6] [7] feet.
 	[End] [and] [center] posts: 3/4 inch face width x 5 inch depth.
	Corner posts: 8 x 8 inches, 90 degree.
 	Top Rail: Not required.
 	Mounting: Surface.
	FINISHES
		Stainless Steel: NAAMM AMP 503; No. 4 satin. 
	EXECUTION
	INSTALLATION	Comment by ZeroDocs: Anchoring schedules and recommendation shall be made by a license structural engineer.

Concrete slab shall be 4000 PSI normal weight, 6 inch minimum thickness, for surface mount stanchion and 8 inch minimum thickness for embedded stanchions. Cracked concrete. lightweight concrete slab,  and corrugated metal deck slabs are not acceptable.
	Install in accordance with manufacturer's instructions and approved Shop Drawings. 	
	Installation Tolerances:
 	Maximum variation from plumb or level: [1/16] [__] inch in 3 feet or [1/8] [__] inch in any 10 feet, whichever is less.
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